## Slide 1: Homo vitro fragilior
Peter G. Wolynes Rice University
AJL @ 80
University of Illinois at Urbana-Champaign
March 2018

## Slide 2
Nonne fragiLIOrES sumus, quam si vitrei essemus? vitrum enim etsi fragile est, tamen servatum diu durat: et invenis calices ab avis et pro avis, in quibus bibunt nepotes et pronepotes.
St. Augustine
Are we not frailer than if we were of glass? For even if glass is fragile, yet if cared for, it lasts a long time and you find grandsons and great-grandsons drinking out of the cups of their grandfathers and great-grandfathers.

## Slide 5: Crystallization vs. Glassy Dynamics
N1/3
crystallite
F
large surface cost
critical nucleus size
Free energy gap
F(N) = -Δƒ N +  N2/3
(ΔEs - TSc),
N
F(N) = - TscN + N1/2
Notice no energy gap.
Crystal nucleation barrier depends on TF - T
Glassy Barrier depends on Tsc alone!
Δ F‡ =
2
4Tsc

## Slide 6
Lubchenko and Wolynes, Annu. Rev. Phys. Chem. 2007, 85:235-66.
Temperature of Vanishing Entropy
Glassy Dynamics from a Mosaic of Energy Landscapes
Super Arrhenius temperature dependence of rates
RFOT theory predicts fragility parameter, m
m from RFOT
m from experiment
Notice no data extrapolation or fitting needed for this comparison.

## Slide 7
Berthier et al. Science (2005) 310, 1797
Data from:
Bohmer et al. J. Chem. Phys. (1993) 99, 4201
RFOT predictions of CPR size agree with experiment

## Slide 10: Prince Rupert’s Drop

## Slide 11
Stress shifts the landscape!
A. Wisitsorasak and PGW 2012

## Slide 12
RFOT Theory Predicts Limiting Strength
of Glasses
A. Wisitsorasak and PGW 2012

## Slide 13
INSERT? . ..

## Slide 14
The Cell is a Marginally Stable Glass
Filamentous network
Structure and shape
Remodeling
Bulk
Polar filaments
track for molecular motors
directed motion
Cytoplasm
Cytoplasmic streaming
Crowded by organelles
W.M. Saxton

## Slide 16: Backup Slides

## Slide 18: Confrontation of Classical RFOT Theory with Observation

## Slide 19: Confrontation of Classical RFOT Theory with Observation
Mobility Transport 2008  rejuvenation front dynamics predicted
Secondary Relaxations 2009  a. nearly Arrhenius
 b. grow in amplitude as Tc is approached
Surface Glass Transitions 2008  halved activation energy
Crystallization Dynamics 2010  new mechanisms of crystal growth and nucleation near Tg

## Slide 20: Some Relationships of RFOT Theory with Other Approaches
RFOT
Theory
(Microscopic) Mode
Coupling Theory
Phenomenological Mode
Coupling Theory
Leutheusser, Götze
Facilitation
Andersen, etc.
Frustrated Phase Transitions- icosahedratics, etc.
Nelson, Kivelson, etc.
Yes, but a higher order effect
Strings,
Bhattacharya,
Bagchi, PGW

## Slide 21: Density of Resonances

## Slide 26: Stevenson and Wolynes, The Ultimate Fate of Supercooled Liquids (2010)
Crystallization and Glassy Dynamics
n n nM
n nM n
region size n
nanocrystallite
Initial amorphous state
The crystal

## Slide 27: Crystallization and the Dynamical Mosaic
Classical
Turnbull Regime
Percolative
Nanocrystallization
Low Temperature
High Temperature
 < M
 > M
M


M


## Slide 28
Stevenson and Wolynes, The Ultimate Fate of Supercooled Liquids (2010)
New Mechanisms of Homogeneous Nucleation emerge near and deep below Tg
When critical crystal nucleus is bigger than dynamically correlated region, percolative nanocrystallization begins.
When nanocrystals percolate fully, complete decoupling of nucleation and growth from  relaxation!
Turnbull
Percolative Nanocrystallization

## Slide 29
Sun et al. J. Phys Chem B, Vol. 112, No. 18, 2008
Stevenson and Wolynes, The Ultimate Fate of Supercooled Liquids (2010)
New Mechanisms of Crystal Growth emerge near Tg
4 orders of magnitude predicted change of crystal growth rate near Tg
3.5 orders of magnitude

## Slide 30: Sun et al. J. Phys Chem B, Vol. 112, No. 18, 2008
Smith et al. American Mineralogist, Vol. 86, 589-600, 2001
Spherulitic Crystallization near and below Tg in the Laboratory and the Field
Time of Formation:
Estimated Time of Formation:
50 years ~ 1022 picoseconds
~ 3m
~ 3 m
5 hours ~ 1017 picoseconds
Silver Cliff District, Colorado
Formed in Late Eocene to Early Oligocene